## Slide 1: TOPCon Solar Cell
Prepared by
Pinal Rana

## Slide 2
Si: 14: 1S2 2S2 2P6 3S2 3P2
Maximum electron in each level: 2n2
1st level: 2*1 = 2
2nd level: 2*22 = 8
3rd level: 2*32 = 18
4th level: 2*42 = 32
Atomic Orbits: S – 2, P – 6, D – 10, F - 14
Cost comparison
Silicon: $ 1.45 – 1.48 /Kg (2nd most abandoned material found from the earth crust)
Germanium: $ 3000 /Kg
Ge: 32: 1S2 2S2 2P6 3S2 3P6 3D10 4S2 4P2
can we make topcon with p type
n type perc is possible
different layer impotance

## Slide 3
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Surface with dangling bond
Surface with dangling bond
Surface with dangling bond
Surface with dangling bond

## Slide 4
N-type base silicon
P+ emitter
N-type base silicon
P+ emitter
Depletion region
No free electron and holes

## Slide 5
N-type base silicon
P+ emitter
Depletion region
No free electron and holes

## Slide 6
N
P
N
P
Rotate 90 degree
anti-clock wise
Band diagram
Valance band
Conduction band
Holes
Electron
Holes are like helium balloons
Electrons are like solid balls
N
P
Holes
Electron
N-

## Slide 7
N
P
Band diagram
Valance band
Conduction band
Holes
Electron
N-

## Slide 8: PERC VS TOPCon
120 nm
60 nm
1-2 nm
The AlOx layer enhances light trapping by acting as part of the reflective coating. This ensures that more sunlight is absorbed by the silicon wafer rather than escaping through the rear.

## Slide 9: Capping layer
Reducing recombination losses via surface and field-effect passivation.
Enhancing light trapping and optical performance.
Protecting against environmental degradation, ensuring long-term stability.
The Al₂O₃ layer enhances light trapping by acting as part of the reflective coating. This ensures that more sunlight is absorbed by the silicon wafer rather than escaping through the rear.
The Al₂O₃ capping layer protects the silicon surface from contamination, oxidation, and exposure to moisture, which can degrade passivation quality over time.
It helps maintain the rear-side passivation quality throughout the cell's lifetime, ensuring minimal efficiency loss.
3 SiH4 (Silane gas) + 4NH3 = Si3N4 + 12H2
hydrogen (H₂) produced during the reaction diffuses into the silicon surface, neutralizing defects.
SiNx has a refractive index typically around 2.0, which is well-suited to minimize reflection and maximize light absorption.
Si∗+H∗→Si-H

## Slide 10: TOPCon VS PERC
Feature | PERC (P-type Silicon) | TOPCon (N-type Silicon)
Light-Induced Degradation (LID) | Suffers from LID due to boron-oxygen defects | No LID; avoids boron-oxygen defects
Efficiency Limit | Lower (22-23%) | Higher (24-25%)
Minority Carrier Lifetime | Shorter | Longer
Cost | Historically cheaper | Slightly more expensive but improving
Stability | Moderate degradation over time | Better stability and longevity
The intensively doped poly silicon layer reveals decent quality of passivation, because of the huge quantity of hydrogen atoms in the poly silicon layer
Passivation Contact Structure: TOPCon cells prepare a super-thin oxide silicon layer (1-2nm) on the back of the silicon wafer, followed by the deposition of a doped polycrystalline silicon layer. This structure not only provides excellent interface passivation but also forms a selective carrier transport channel, allowing majority carriers (electrons) to pass through while preventing minority carriers (holes) from recombining, thus significantly increasing the cell's open-circuit voltage (Voc) and fill factor (FF).

## Slide 11: TOPCon
1. Energy Band Diagram
TOPCon introduces a thin tunnel oxide layer and a doped polycrystalline silicon (poly-Si) layer on the rear surface of the solar cell. This structure modifies the energy band alignment, enabling the efficient flow of electrons while blocking holes.
Tunnel Oxide Layer:
  Acts as a potential barrier for charge carriers (electrons and holes).
  Quantum tunnelling allows electrons to pass through this extremely thin layer (~1–2 nm).
Poly-Si Layer:
  The poly-Si layer aligns energetically with the silicon substrate, enabling carrier selectivity:
    It allows electrons (majority carriers) to pass through.
    It blocks holes (minority carriers) from recombining.

## Slide 12
a. Passivation
Surface Recombination: At a silicon interface, defects (dangling bonds) act as recombination centers where electrons and holes annihilate, reducing efficiency.
Tunnel Oxide Passivation:
  The SiO₂ layer passivates the silicon interface, reducing the number of surface defects and suppressing recombination losses.
  Passivation improves the effective carrier lifetime.

## Slide 13
b. Quantum Tunneling
The tunnel oxide layer is extremely thin (~1–2 nm), enabling quantum mechanical tunneling of electrons.
Quantum Tunneling:
  Electrons can penetrate the potential barrier (oxide layer) even though classical physics suggests they shouldn’t.
  This happens because of the wave-like nature of electrons in quantum mechanics.
Electrons generated in the silicon substrate can "tunnel" through the oxide layer into the poly-Si layer, reaching the contact for collection.
Holes, due to their higher effective mass and energy alignment, are blocked.

## Slide 14
c. Carrier Selectivity
Carrier selectivity is achieved using the doped polycrystalline silicon layer:
  For N-type TOPCon cells, the poly-Si is heavily phosphorus-doped.
  This layer selectively allows electrons to pass through while repelling holes (due to band bending and electric fields).
This selective contact ensures that only electrons reach the rear contact, reducing recombination losses further.

## Slide 15
3. Energy Band Alignment
The energy band diagram of TOPCon illustrates:
The tunnel oxide forms a potential barrier for holes while allowing electrons to tunnel through.
The poly-Si layer introduces an electric field that assists in separating charge carriers efficiently.
As a result:
  Electrons are collected at the rear contact (improving efficiency).
  Holes are blocked, minimizing recombination.

## Slide 16
4. Why N-Type Silicon Works Better in TOPCon
From a physics perspective, N-type silicon offers:
Higher carrier lifetime: Fewer defects and recombination losses.
No Light-Induced Degradation (LID): Unlike P-type silicon (boron-doped), N-type silicon avoids boron-oxygen defects.
Better Tunneling Properties: N-type substrates align better with the poly-Si layer for tunneling.

## Slide 17
Phosphorus-doped polysilicon (poly-Si) is negatively charged because it has free electrons. However, the movement of electrons from the N-type silicon wafer to the phosphorus-doped poly-Si is not due to attraction.
Energy band alignment
Quantum tunneling